## Slide 1: Machine Learning Examples in 2D Material Development
Collaboration - 02 Meng-Chi (Ed) Chen NMEG, 2026-06-18
Machine-Learning-Driven Numerical Analysis of SEM Images
for Optimizing MOCVD-Grown MoS₂ Device Performance
Dimension:2.4, 31.5
Position: 1, 0.5
Recipe
Synthesis
Sample
SEM Image
Characterization
Device
Fabrication
Performance
Measurement
SEM Image Numerical Representation
Coverage calculation ✓
Scale mark extraction ✓
Average grain size calculation ✓
Nucleation density calculation ✓
Circumference calculation ✓
Background noise representation ✓
Computer Vision
Analysis
Prediction
Recipe Optimization
✓
△
△
Notes: The exploration of two-dimensional (2D) materials for next-generation semiconductors begins with recipe optimization to synthesize high-quality 2D materials
, followed by characterization such as optical microscopy, Raman spectroscopy, atomic force microscopy (AFM), and scanning electron microscopy (SEM).
Samples with promising quality proceed to device fabrication and performance testing.
From experience, we (Jiadi) find that scanning electron microscopy (SEM) images strongly correlate with device outcomes.
However, a systematic numerical description of SEM results is lacking.
Here, we present an algorithm that leverages machine learning and computer vision to provide a numerical representation (NR) of SEM images of 2D MoS₂, correlating this NR with device performance and using the desired NR for recipe optimization .
This research is ongoing, with a green checkmark indicating completed functions and a yellow triangle highlighting areas still under development.
Today, I would like to show you the current stage of this project.

## Slide 2: Project Control Table
.
Dimension:3, 31.8
Position: 1, 0.5
Content | Brief | Type | Link
TMD CV Analysis | SEM data | Dropbox | https://www.dropbox.com/scl/fo/36wrwwr47m0vifwe8wvnu/AF0F0pOW3Z0kwe34LtRxTuM?rlkey=2v16wbs3bq6vu81e4fph4nnok&st=ibc5brxd&dl=0
MoS2 Material and Performance Characterization | Exp recipe | Google Sheet | https://docs.google.com/spreadsheets/d/1oJ1RdsqrisFb9jxFJyc4TyQTLStmKBVbRIwYu-NxrmI/edit?usp=sharing
2024-0828_SEM Image Seg | Presentation | .pptx | https://mitprod-my.sharepoint.com/:p:/g/personal/edchen93_mit_edu/EeBhIB1nFoVAlkqaQcClEtsBsYqwneUawGiF3oEFSIJpbg?e=pXUIMv

## Slide 3
3 hr
1 hr
Ignore
NA.
Notes: 2024-12-02
Consider other factors.

## Slide 4: How to describe an SEM image of a 2D material?
Coverage: Percentage of area covered by crystal. (Unit: %)
Grain size: Size of individual crystal. (Unit: )
Nucleation density: Number of crystal in unit area. (Unit: )
Shape: Shape of crystal.
Impurity: Precursor residuals or other small crystals.
Orientation: Direction of crystals.
… More
Dimension:3, 31.8
Position: 1, 0.5
How to get these information?
ImageJ (or other scientific software for microscopic image processing)
  Require multiple steps of settings and adjustments. ✗
  Some of our desired function are not exist (or require excessive post process). ✗
Python
  Customize the field-specific needs. ✓
  Streamline the process. ✓
Notes: How do we usually describe an SEM image of a 2D material?

## Slide 5: Execution Steps
Pixel per um (sclbar_text, pixel_length_sclbar, pixels_per_um).
Coverage (pct_black, pct_white).
Segmentation Images (cnt_seg_success)
Nucleation density (nd_per_sqnm)
Grain size (avg_gs_squm, std_gs_squm)
Circumference (avg_circumf_um, std_circumf_um)
Cricumference Square to Area Ratio (avg_csar, std_csar)
Background noise (avg_bkgd_pixel, std_bkgd_pixel)
Extract scale bar info from SEM image.
Convent SEM image to grayscale.
Crop out the center square.
Enlarge image for better CV processing (cv2.INTER_LINEAR).
Slightly blur the image (cv2.medianBlur(k=5)).
Enhance image (CLAHE and merge).
Binarize image with Otsu's method.
Calculate coverage and create histogram.
Watershed image.
Segment image and save segmentations.
Calculate segmentation result.
Save result as excel.
Dimension:3, 31.8
Position: 1, 0.5
enh_cliplmt=2, enh_tileGrid=8
Numerical Representation
Computer Vision Analysis of 2D Material SEM Image

## Slide 6: How are these measurements relating to devise performance?
Numerical representation of 2D material SEM images:
Pixel per um (sclbar_text, pixel_length_sclbar, pixels_per_um).
Coverage (pct_black, pct_white).
Segmentation (cnt_seg_success)
Nucleation density (nd_per_sqnm)
Grain size (avg_gs_squm, std_gs_squm)
Circumference (avg_circumf_um, std_circumf_um)
Cricumference square to area ratio (avg_csar, std_csar)
Background noise (avg_bkgd_pixel, std_bkgd_pixel)
Device
Performance
Dimension:3, 31.8
Position: 1, 0.5
It might be harder to see the relation of one single measurement relates directly to the device performance.
ML model can help correlate measurements from SEM image to device performance when there is more data.

## Slide 7: Demo Video
Dimension:3, 31.8
Position: 1, 0.5
Original
Gentle Blurred
Gentle Enhanced
Binarized
Single folder SEM image segmentation.
Took 2 mins to process 4 images.
[OneDrive] Image Seg Demo_480p.mp4
[Local] Image Seg Demo_1080p.mp4

## Slide 8
Auto Scale Bar Extraction
Average pixel in columns and rows to cut out desired area of scale bar.
Use pytesseract to read the number of the scale bar.
The length of scale bar matches the actual pixel checked with Photoshop.

## Slide 9: Coverage
Original
Gentle Blurred
Gentle Enhanced
Binarized
Dimension:3, 31.8
Position: 1, 0.5
Original
Gentle Blurred
Gentle Enhanced
Binarized
Otsu's method of thresholding: minimizing the intra-class variance.
Ed: TM92_C-Sapp_02

## Slide 10: Otsu’s Method
Otsu's method selects a threshold that maximizes the between-class variance . (Or equivalently, minimizing intra-class intensity variance.
and are standard deviation and variance between groups, respectively.
and are proportion of pixels in background and foreground respectively, and .
Dimension:3, 31.8
Position: 1, 0.5
otsu_threshold, arrimg_5bnrz \
= cv2.threshold(arr_img, 0, 255, cv2.THRESH_BINARY + cv2.THRESH_OTSU)

## Slide 11: Watershed
Prepare image: grayscale, noise reduction, then binarize.
Identify background by dilating (extend edge a little bit) the binary image.
Apply distance transform that turn none-zero pixel into the distance to nearest black pixel.
Set threshold to make out foreground from the distance transform result.
Subtract foreground from background to create unknown regions
Apply watershed by flooding between foreground islands to cut though unknown regions.
Dimension:3, 31.8
Position: 1, 0.5
分水嶺
Prepared image
Background
Distance Transform
Foreground
Unknown
Watershed
Cut through crystals that sticks together.

## Slide 12: Distance Transform
Distance Transform applied to a binary image so that:
Black (0) regions remain black, representing the background.
White (non-zero) regions are transformed so each pixel's value represents the distance (in pixels) to the nearest black (0) pixel.
Dimension:3, 31.8
Position: 1, 0.5
分水嶺
Input image
After distance transform

## Slide 13: Watershed Parameter Adjustments
frgd_thrs_ratio is a parameter between 0 and 1 that controls the erosion from the edge of foreground.
Dimension:3, 31.8
Position: 1, 0.5
0.3
0.4
0.5
0.6
0.7
Linked error
Missing error
0.45
Too high, some foregrounds are missing.
Too small, some foregrounds are linked together.
It’s hard to find a middle ground that both error won’t occur.
Setting suitable for this image might not be suitable for another image.

## Slide 14: Watershed Improvement — Add foreground at local maxima
Dimension:3, 31.8
Position: 1, 0.5
After distance transform
Original
Mark local maxima
Move a searching window through the image to find local maximum.
If a maximum is found, mark it with white, so that it will be recognized as a foreground (island) in the later watershed.

## Slide 15: Foreground Sharp Edge Smoothing
Some crystal have sharp edge that during foreground extraction, a single crystal will become multiple crystals, causing error in the later watershed.
Solution: Applied edge smooth to the extracted foreground, then proceed watershed.
Dimension:3, 31.8
Position: 1, 0.5
Input
Foreground/Background overlay
Normal case.
This issue case.
Corrected result.

## Slide 16
Dimension:3, 31.8
Position: 1, 0.5
Original
Gentle Blurred
Gentle Enhanced
Binarized
(a) Image process: Crop, enlarge, blur, enhance, and watershed.
(b) Before segmenting (last of image process).
(c) Segmentation result (layer by layer).
(d) Segmentation result (overlap).
(e) Precessing terminal
Segmentation Approach with more reliable traditional segmentation process.
(a)
(b)
(c)
(d)
(e)
(f)
(g)

## Slide 17: Future Work
Improve the watershed function to better adapt to SEM images in various condition.
Obtain device data from Jiadi or Yixuan to correlate the numerical representations of SEM images with device performance.
Conduct literature research on the feasibility of using machine learning models to embed SEM images into dense array representations.
Dimension:3, 31.8
Position: 1, 0.5
Recipe
Synthesis
Sample
SEM Image
Characterization
Device
Fabrication
Performance
Measurement
SEM Image Numerical Representation
Coverage calculation ✓
Scale mark extraction ✓
Average grain size calculation ✓
Nucleation density calculation ✓
Circumference calculation ✓
Background noise representation ✓
Computer Vision
Analysis
Prediction
Recipe Optimization
✓
△
△

## Slide 18
512x512
128x128
32x32
8x8

## Slide 19: Future Work Calibri Light, 20-24 Normal
Crystal Violet
Patent
Mobility data (B620 ~B640)
Dimension:3, 31.8
Position: 1, 0.5

## Slide 20: Calibri Light, 32-36, Bold (H=2.8, W=30, x=1, y=0.5) Calibri Light, 20-24 Normal
Calibri, 16-24, Normal (H=13, W=30, x=1, y=3.8)
Calibri, 16-24, Normal (H=13, W=30, x=1, y=3.8)
Dimension:3, 31.8
Position: 1, 0.5

## Slide 21: Future Work Calibri Light, 20-24 Normal
Crystal Violet
Patent
Mobility data (B620 ~B640)
Dimension:3, 31.8
Position: 1, 0.5